## Slide 1
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 2
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity
2. Film quality, voiding, seams, or residues
3. BEOL Aluminum etch / CMP interaction
4. Slot tracking and wafer sequencing validation
5. FA cross-section confirmation
Generated from JSON analysis

## Slide 3
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 4
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 5
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 6
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 7
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 8
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 9
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 10
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 11
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 12
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 13
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 14
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 15
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 16
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 17
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 18
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 19
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 20
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 21
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 22
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 23
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 24
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 25
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 26
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 27
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 28
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 29
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 30
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 31
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 32
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 33
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 34
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 35
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 36
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 37
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 38
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 39
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 40
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 41
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 42
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 43
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 44
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 45
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 46
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 47
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 48
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 49
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 50
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 51
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 67
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 52
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 53
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 54
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 55
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 56
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Film quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 57
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 58
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Single wafer excursion with elevated Rc and 100% ViaFQ opens indicates localized BEOL failure rather than systematic lot issue. Evidence points to slot-specific abnormality through W deposition (abort/long delay) with consistent slot tracking from FQ etch through downstream steps. Wafer mapping behavior suggests possible mis-tracking after W dep, but physical defect propagation aligns with BEOL Aluminum process sensitivity (etch/CMP/deposition interaction). Likely electrical signature driven by contact/via interface degradation rather than full opens.
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 59
Recommended Investigation Path
Recommendation
Focus on W deposition event integrity and downstream BEOL Aluminum module interactions. Investigate whether W dep abort or delay induced film quality degradation (voiding, seam formation) impacting via/contact resistance. Cross-check BEOL oxide etch and CMP steps for over/under process coupling with via profile integrity. Validate slot-specific handling and wafer tracking accuracy to rule out misprocessing. Prioritize FA cross-section to confirm via/contact interface condition and identify metallization discontinuities or contamination.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 60
Action Plan
Owner | Action | Due Date
BEOL Integration | Correlate W dep abort/delay logs with film quality metrics and check for pedestal/tool-specific anomalies impacting slot 2 | 2026-07-01
Process Engineering | Review BEOL Aluminum etch and CMP uniformity for over/under-process conditions affecting via/contact resistance | 2026-07-03
Failure Analysis | Perform FIB cross-section on failing wafer to confirm via fill integrity, interface condition, and presence of voids or residues | 2026-07-02
Manufacturing Ops | Validate slot tracking consistency post W deposition to ensure no misalignment or wafer mis-sequencing occurred | 2026-07-01
Generated from JSON analysis

## Slide 61
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 62
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 63
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 64
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 65
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 66
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 67
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 68
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 69
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 70
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 71
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 72
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 73
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 74
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 75
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 76
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Localized BEOL failure signature with slot-specific abnormality and likely contact/via interface degradation.
Generated from JSON analysis

## Slide 77
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 78
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 79
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
Not specified
Generated from JSON analysis

## Slide 80
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 81
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 82
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Bad test signal in SIGE9HP with FEOL/BEOL mismatch is most consistent with BEOL copper-related electrical degradation rather than FEOL device failure. Prior BLIPS data shows similar signatures driven by Cu CMP overpolish causing loss of contact and SA nitride deposition conditions leading to excess Cu silicide formation and elevated resistance. These mechanisms are often tool/sequence dependent and wafer-position sensitive, indicating process-induced variability rather than intrinsic FEOL defectivity. [1][2]
Confidence: Medium
Primary Failure Interpretation
xyz example failure interpretation for BEOL copper integration
Generated from JSON analysis

## Slide 83
Recommended Investigation Path
Recommendation
Focus investigation on BEOL copper integration modules, specifically CMP endpoint control, cap nitride deposition sequencing, and tool conditioning effects. Correlate electrical failures to wafer position, recent tool maintenance/recipe changes, and multi-lot common tool usage. Validate whether signal is driven by contact resistance increase or open behavior before engaging FEOL RCA.
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 84
Action Plan
Owner | Action | Due Date
INTG Team | Perform wafer-level correlation of failing signal vs. CMP endpoint metrics and check for overpolish signatures | 2026-07-01
BEOL Module Engineer | Review recent SA nitride deposition runs for chamber conditioning, RF reflected power, and sequence after clean recipes | 2026-07-01
Yield/Characterization | Analyze electrical parametrics (Rline, via/contact resistance) to confirm Cu resistance shift vs. open failure mode | 2026-06-30
Process Integration | Identify common tools across impacted lots and cross-check for maintenance, aborts, or rework events | 2026-07-02
Generated from JSON analysis

## Slide 85
BEOL Excursion Summary
Rc Elevation and ViaFQ Opens — JSON Generated Report
Executive Summary
Yield loss on Bipolar_MBXP_NPN_CBEBC_Nom_BVcbo shows degradation between M2 and LM on identical sites, indicating parametric shift rather than intrinsic defectivity. Signature aligns with prior known test-induced degradation mechanisms impacting NPN structures.
Confidence: High
Primary Failure Interpretation
Electrical overstress / measurement-induced damage at M2 causing degradation of BVcbo and Vbe at LM, not baseline FEOL defectivity
Generated from JSON analysis

## Slide 86
Recommended Investigation Path
Recommendation
Isolate test-induced damage vs process defect by re-testing fresh sites and cross-checking M2 vs LM deltas; implement test condition review and limit stress exposure on sensitive NPN structures
Key Focus Areas
1. W deposition abort / delay integrity 2. Fil quality, voiding, seams, or residues 3. BEOL Aluminum etch / CMP interaction 4. Slot tracking and wafer sequencing validation 5. FA cross-section confirmation
Generated from JSON analysis

## Slide 87
Action Plan
Owner | Action | Due Date
Test Engineering | Review M2 test conditions and probe stress levels impacting BVcbo-sensitive structures | 2026-07-05
Characterization | Run split test (fresh vs previously tested sites) to confirm measurement-induced degradation | 2026-07-07
Integration | Validate no FEOL process excursions by comparing to recent baseline lots with same flow | 2026-07-08
Generated from JSON analysis